MIPOLAM PLANET

MIPOLAM PLANET™ is fully flexible homogeneous compacted floorcovering in sheet, 2m wide, providing excellent resistance to wear and tear in high traffic areas. Their weight is 2700 gr/m².

They feature a non-directional design incorporating translucent chips that provides a 3D effect and ensures an even colour throughout the thickness presenting a nice matt finish over 40 colours.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as betadine, eosin, hydro alcoholic solutions, making the maintenance easy and the floor long lasting. This treatment avoids applying any acrylic emulsion throughout the lifetime of the product. 
It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio  accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant. It is 100% phthalates free and recyclable.
Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class).

According to ISO 21702, Mipolam Planet has anti-viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Planet has anti-bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

The flooring is antistatic (<2kV), its residual indentation is ≈ 0.02 mm.

The flooring complies with the EN ISO 10581 norm, has a binder content Type I and is suitable for heavy duty traffic areas and Bfl-s1 fire resistance.

As part of our sustainable development policy, this product is manufactured in the first floor covering plant awarded with the triple certification: ISO 9001 (quality),

ISO 14 001 (environment) and OHSaS 18001 (safety).