Specification

# Combo’Clad

Adhesive protection plates – 200 or 150 mm high

- Description : adhesive protection plate (Combo’Clad 200 or 150 as manufactured by SPM) from slightly textured (Optimixt grain as manufactured by SPM) and antibacterial PVC achieving Bs2d0 fire rating with solid colour. PVC profile is 200 or 150 mm high and 3 mm thick. It is provided with 3 strips of foam adhesive tape for fixing (or without adhesive tape on request).

- Environment: no heavy metals and no substance potentially subjected to any REACH restriction are used in its manufacture, nor PBT/BPA. The calcium-zinc thermal stabilisation process is used. The emission level of volatile substance in inside air has been tested according to ISO 16000-6 and is very low (A+) according to the French regulation (23 March 2011 nr 2011-321 Decree and 19 April 2011 Order). 100% of the product are recyclable.

- Colour: selected by architects from manufacturer’s standard range.

- Installation method: adhesive. SPM universal mastic glue is recommended for stronger fixing.