GRADUS Brickworks is a textile, decorative, antistatic floorcoverings available in tiles 50x50cm. It consists in a 800g/m² tufted structured loop pile layer of 100% solution died INVISTA polyamide 6.6 on a non-woven polyester backing and  a stabilized bitumen backing. The overall thickness is 6.5mm.

It has a very good wear resistance thanks to its 254880 points/m² and an impact sound insulation ΔLw=25dB.

GRADUS Cityscene is a looselay floorcovering with a Bfl-s1 class for smoke emission according to EN 13501-1.