GRADUS LAFITE CONNECT PLAINS, STRIPES & DESIGN.

GRADUS Lafite Connect Plains, Stripes and Design are  textile, decorative, antistatic floorcoverings available in tiles 50x50cm. It consists in a 540g/m² tufted loop pile layer of 100% solution died nylon AQUAFIL on a non-woven polyester backing and  a stabilized bitumen backing. The overall thickness is 5,9mm.

GRADUS Lafite Connect Plains, Stripes, Design have a very good wear resistance thanks to its 170602 points/m² and an impact sound insulation ΔLw=22dB.

GRADUS Lafite Connect Plains, Stripes, Design are  looselay floorcoverings with a Bfl-s1 class for smoke emission according to EN 13501-1.