GRADUS Urban Myth is a textile, decorative, antistatic floorcoverings available in tiles 50x50cm and planks 25x100cm. It consists in a 650g/m² tufted loop pile layer of 100% solution died ANTRON LUMENA Nylon 6.6 on a non-woven polyester backing and  a stabilized bitumen backing. The overall thickness is 6mm.

It has a very good wear resistance thanks to its 205320 points/m² and an impact sound insulation ΔLw=23dB.

GRADUS Urban Myth is a looselay floorcovering with a Bfl-s1 class for smoke emission according to EN 13501-1.