MIPOLAM ACCORD EL7

MIPOLAM ACCORD EL7 is a dissipative flexible homogeneous vinyl floorcovering available in both sheet and tile form, calendered and compacted and comes in 6 colours.

This floorcovering is treated with Evercare™: the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. Evercare™ avoids stain of chemical products used in healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics; it requires no wax for life!

MIPOLAM ACCORD EL7 acts as a continuous dissipater 106 ≤ Rt ≤ 108. It has permanent antistatic properties (< 100 V).

The product is non-reactive to residual indentation with a value ≤ 0,02 mm.

The flooring has a binder content type II, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.

The product is non-emissive of volatile organic compounds with <10 µg/m3 (TVOC after 28 days ISO 16000-6).