MIPOLAM ESPRIT

MIPOLAM ESPRIT is a vinyl flooring homogeneous pressed in 2m sheets, with a thickness of 2mm and a weight ≤ 2780 g.

The non-directional design with colour throughout the thickness is available in 24 references presenting a nice matt finish.

This flooring is suitable for heavy duty traffic areas, and facilitates floor–wall junctions, angles and welding treatments.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as Betadine, eosin, hydro alcoholic solutions, making the maintenance easy and long lasting the flooring.

This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is composed of 45% minerals, 22% of inexhaustible material and at least 25% of recycled 100% controlled. It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant.

COV emissions after 28 days (ISO 16000-6) are below detection levels

with <10 μg / m3 and this product is classified A + (the best class).

MIPOLAM ESPRIT is 100% phthalate free and 100% recyclable.

The flooring is antistatic (<2kV), its residual indentation is ≤ 0.02 mm.

The flooring is compliant with EN ISO 10581 and has a binder content Type I, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.