Mipolam Biostyl / Styl

Mipolam Biostyl™ and Mipolam Styl are a fully flexible compacted floorcovering in sheet, 2m wide, abrasion group T, providing excellent resistance to wear and tear in high traffic areas. Its weight is 2630 gr/sqm. It features a non directional design incorporating coloured transparent chips to ensure an even colour throughout the thickness.

This floorcovering is recommended for private and administrative buildings and thanks to its great flexibility it simplifies the installation of bend-up skirting, as well as angles and hot welding procedures.

This floorcovering is treated with Evercare™ or the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. Evercare™ avoids staining of chemical products used in healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics; it requires no wax for life!

According to ISO 21702, Mipolam Symbioz has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Symbioz has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

Mipolam Biostyl™ contains over 75% sustainable or renewable raw materials. It includes a 100% bio based plasticizer, made of residues from cereals (wheat,

corn…) and REACH compliant.

This floorcovering has extremely low VOC emissions, more than 40 times lower than the European standards ( <10 µg/m3 TVOC after 28 days ISO 16000-6).

This floorcovering is anti-static (<2kV), inhibits the growth of bacteria and resistant to the main chemical products used in healthcare and is non-reactive to residual indentation with a value ≤ 0,02 mm (EN 433).

Mipolam Biostyl is available in 25 fashionable and relaxing colours.

As part of our sustainable development policy, this product is manufactured in a plant certified with highest quality standards iSO 9001 and environmental standards iSO 14 001.