MIPOLAM SYMBIOZ

MIPOLAM SYMBIOZ™ is fully flexible homogeneous compacted floorcovering in sheet, 2m wide, providing excellent resistance to wear and tear in high traffic areas. Their weight is 2595 gr/m².

They feature a non-directional design incorporating coloured chips to ensure an even colour throughout the thickness presenting a nice matt finish.

Comprising 83% natural and recycled content, including 17% bio content, 45% mineral raw material (Salt & chalk) and 21% recycled content, MIPOLAM SYMBIOZ™ achieves a 20% to 30% reduction in Cradle to Gate CO2 emissions compared to standard homogeneous flooring.It is 100% phthalates free and recyclable.

This floorcovering is a non-emissive product (below the level of VOC measurement accuracy).

According to ISO 21702, Mipolam Symbioz has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Symbioz has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as Betadine, eosin, hydro alcoholic solutions, making the maintenance easy and long lasting the flooring.

This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

The flooring is antistatic (<2kV), its residual indentation is ≈ 0.02 mm.

The flooring complies with the EN ISO 10581 norm, has a binder content Type I and is suitable for heavy duty traffic areas and Bfl-s1 fire resistance.

As part of our sustainable development policy, this product is manufactured in the first floor covering plant awarded with the triple certification: ISO 9001 (quality),

ISO 14 001 (environment) and OHSaS 18001 (safety).