Mipolam Troplan

MIPOLAM TROPLAN is a vinyl flooring homogeneous calendered and pressed in 2m sheets, with a thickness of 2mm and a weight ≤ 3300g.

The directional design with colour throughout the thickness is available in 18 references presenting a nice matt finish.

This flooring is suitable for medium to high traffic areas, and facilitates floor–wall junctions, angles and welding treatments.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as Betadine, eosin, hydro alcoholic solutions, making the maintenance easy and long lasting the flooring.

This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is composed of 45% minerals, 22% of inexhaustible material and at least 25% of recycled 100% controlled. It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant.

According to ISO 21702, Mipolam Troplan has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Symbioz has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

Mipolam Troplan is 100% recyclable.

COV emissions after 28 days (ISO 16000-6) are below detection levels with <10 μg / m3 and this product is classified A + (the best class).

MIPOLAM TROPLAN is 100% phthalate free.

The flooring is antistatic (<2kV), its residual indentation is ≤ 0.03 mm.

The flooring is compliant to the EN ISO 10581 norm, has a binder content type II, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.