**PREMIUM COMFORT**

The floor covering is made of a **>1mm thick, pure vinyl homogeneous wear layer with no filler, incorporating very densely pressed coloured chips**, with a **mat finishing** and **without a transparent wear layer**.

It offers a T group wear rating and is available in 2 m wide sheet. The product contains a compact backing which is calendered, pressed and a Very High Density (VHD) foam backing. It is reinforced with a double glass fibre grid.

It offers a **16 dB sound insulation, an indentation resistance of 0.06 mm and a rolling heavy loads easiness**.

**PREMIUM COMFORT** is treated with **Evercare™**, a surface treatmentobtained by UV laser crosslinking. It ensures easy maintenance and eliminates permanently the need for acrylic emulsion (metallisation). It avoids staining of chemical products used in healthcare like iodine alcohol, Betadine, eosin and anti-bacterial hand gel.

According to ISO 21702, **TARALAY PREMIUM** **COMFORT** has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, it has anti bacterial activity against E. coli, S. aureus and MRSA of 99% after 24h00.

It is 100% compliant with REACH.

It is composed of 40% of minerals and inexhaustible materials.

It is made with more than 50% recycled content ; 100% of which are fully controlled and REACH compliant.

It does not contain any heavy metals, any formaldehydes and it is made with phthalate free plasticizers

The products emission rate of volatile organic compounds is **<10µg/m3 (TVOC after 28 days – ISO 16000-6).**

It is 100% recyclable.