TARALAY EMOTION is a multilayered compact vinyl floorcovering, available in 2m wide sheet, with a group T wear rating.

The product comprises a printed design that is protected by a transparent wear layer (0.70 mm thick)and a compact backing with fiber glass reinforced layer, which resists against static or dynamic perforation under rolling loads and provides good dimensional stability.

TARALAY EMOTION is protected by a UV cured surface treatment Protecsol® which facilitates ease of maintenance and eliminates permanently the need of an acrylic emulsion (metallisation).

It does not contain any heavy metals or CMR 1&2 and it is 100% compliant with REACH. The product emission rate of volatile organic compounds is < 100 µg/m3 (TVOC after 28 days – ISO 16000 -6). It is 100% recyclable.