TARALAY IMPRESSION COMFORT 0,65 is an acoustic multi-layered vinyl floorcovering, available in 2m wide sheet, with a group T wear rating.

The product comprises a Very High Density (VHD) foam backing reinforced with a glass fibre and a printed design that is protected by a transparent wear layer (0.65 mm thick). It offers 19 dB sound insulation and an indentation resistance of  ca. 0.08 mm.

The flooring is equipped with Protecsol® 2, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as betadine, eosin, hydro alcoholic solutions, making the maintenance easy and the floor long lasting. This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio  accumulative) or PBT (persistent, bio-accumulative and toxic) and is 100% REACH compliant.
Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class) and Floorscore® & M1 certified for indoor air quality. Taralay Impression Comfort Plus has antibacterial efficacy (E.coli / S.aureus / MRSA) : > 99% after 24 hours according to ISO22196.