TARALAY PREMIUM DRY-TEX SYSTEM includes TARALAY PREMIUM DRY TEX and GERPUR glue.

This system provides a complete moisture mitigation in full-spread adhesive installation eliminating interposition barrier for any slab with high moisture (up to 98%RH).

TARALAY PREMIUM DRY-TEX is a multi-layered calendered and pressed vinyl floorcovering, with no filler and a group T wear rating, available in 2m wide sheet.

The product comprises a >1mm thick homogeneous, pure vinyl wear layer incorporating very densely pressed coloured chips, with a mat finishing and without transparent wear layer.

The product comprises a 100% post-manufacturing compact reinforced with a glass fiber grid and a non-woven backing. The product offers 8dB sound insulation, an indentation resistance of 0.03mm and a rolling heavy loads easiness.

TARALAY PREMIUM DRY-TEX is treated with Protecsol®2, a surface treatment obtained by UV laser crosslinking. This Protecsol®2 ensures easy maintenance and eliminates permanently the need for acrylic emulsion (metallisation). It avoids staining of chemical products used in healthcare like iodine alcohol, Betadine, eosin and anti-bacterial hand gel.

According to ISO 21702, TARALAY PREMIUM DRY-TEX has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, it has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

It is composed of 40% of minerals and inexhaustible materials.

It is made of 100% controlled recycled materials.

It does not contain any heavy metals or CMR 1&2 and they are 100% compliant with REACH.

The products emission rate of volatile organic compounds is <10µg/m3 (TVOC after 28 days – ISO 16000-6).

It is 100% recyclable.