TARALAY UNI COMFORT is an acoustic multi-layered vinyl floorcovering, available in 2m wide sheet, with a group T wear rating. The product comprises a Very High Density (VHD) foam backing reinforced with a glass fibre and a calendered wearlayer with colour within the 0,65mm thickness.

It offers 17 dB sound insulation and an indentation resistance of ca. 0.11mm. It has a plain coloured design, making it ideal for cut design work. It is protected by a UV cured surface treatment Protecsol® which facilitates ease of maintenance and eliminates the need of an acrylic emulsion (metallisation).

It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio  accumulative) or PBT (persistent, bio-accumulative and toxic) and is 100% REACH compliant.
Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class) and Floorscore® & M1 certified for indoor air quality. Taralay Impression has antibacterial efficacy (E.coli / S.aureus / MRSA) : > 99% after 24 hours according to ISO22196.