Tarasafe Ultra & Geo

TARASAFE ULTRA & GEO are slip resistant vinyl floorcoverings, with a PVC wear layer and deeply inlaid mineral crystal particles (patented) and coloured chips (Tarasafe Ultra) for a decorative design.

There are reinforced with a glass fibre grid in sheet form.

They are treated with SparClean® surface treatment, a low maintenance cost effective solution providing extreme resistance from soiling and staining.

According to ISO 22196, they have an anti bacterial activity against MRSA of 99% after 24h00.

They are an ideal solution for heavy traffic applications where enhanced slip resistance, durability, hygiene and easy maintenance are required. Tarasafe is suitable for most commercial and industrial areas, with a 12 year warranty.

They do not contain any heavy metals or CMR 1&2 and are 100% compliant with REACH. The products emission rate of volatile organic compounds is < 100 µg/m3 (TVOC after 28 days – ISO 16000 -6). These products are 100% recyclable.