ARCHITECTON

ARCHITECTON is a flexible monolayer homogeneous calendered flooring with a thickness of 2 mm and a weight of ≤ 3680 g. The directional design with colour throughout the thickness is available in 19 tile references.

This flooring is anti-static (< 2 kV), non reactive to residual indentation with a value ≤ 0,03 mm (EN 433).

It receives a protective PU factory seal: a good foundation for routine maintenance. Acrylic emulsion / polishes is required after installation.

The flooring complies with the EN 649 (33-42) offering a group F wear rating suitable for normal to medium traffic areas.

The product emission rate of volatile organic compounds is < 10 μg/m3 (TVOC after 28 days ISO 16000-6).