Mipolam EL7

MIPOLAM EL7 is a dissipative flexible homogeneous vinyl floorcovering available in both sheet and tile.

The 2 mm homogeneous material is calendered and pressed. It has permanent antistatic properties (< 100 V). It acts as a continuous dissipative 10^6 < Rt < 10^8 (EN 1081).

This floorcovering is treated with Evercare®: the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. Evercare® avoids stain of chemical products used in healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics; it requires no wax for life!

According to ISO 21702, Mipolam EL7 has anti-viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam EL7 has anti-bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

MIPOLAM EL7 acts as a continuous dissipative 10⁶ ≤ Rt ≤ 10⁸. It has permanent antistatic properties (< 100 V). The product has to be grounded with an ESD copper strip (cf. finishes) to meets its full performance.

It is 100% phthalate free.

The product is non-reactive to residual indentation with a value ≤ 0,02 mm (EN ISO 24343-1)

The flooring complies with the EN ISO 10581 offering a binder content type II, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.

The product is non-emissive of volatile organic compounds with <10 µg/m3 (TVOC after 28 days ISO 16000-6).