DECOKID

# DECOKID

# Protection and educational panel

Description wall protection and educational panel (Decokid educational panel as manufactured by Gerflor) from rigid, antibacterial and translucent PVC achieving Bs2d0 fire rating with a visual printed on the back. The surface is lightly textured. Its width is 0.75 m, height 1.30 m and thickness 1 mm.

No heavy metals and no substance potentially subjected to any REACH restriction are used in its manufacture. The calcium-zinc thermal stabilisation process is used. The emission level of volatile substance in inside air has been tested according to ISO 16000 and is under 15μg/m3.100% of the product are recyclable.

Colour: selected by architects from manufacturer’s standard range.

Installation sequence: Universal mastic glue as per manufacturer’s instructions.